## Slide 1
University of Larbi Ben M'hidi Oum El Bouaghi
Faculty of Earth Sciences and Architecture
Department of Geology
Crystallography
Licence Geology
2nd year Common core
By SAADALI Badreddine
Course VI-3

## Slide 2
Course VI-3
Crystal structure anomalies

## Slide 3
Anomalies or defects in crystal structures can significantly influence the properties of minerals. Irregularities in the spatial arrangement of atoms in an ideal infinite crystal lead to crystalline defects which increase the energy of a solid that would otherwise be in stable equilibrium for a periodic crystal structure. These structural defects are categorized into three types:
Point defects, which are on the scale of an atomic volume;
Linear defects or dislocations, which are disturbances in the crystal structure along a line of atoms or a lattice row;
Two-dimensional or planar defects, which primarily involve imperfections at interfaces separating two crystals.
Crystal structure anomalies

## Slide 4
Crystal lattices are altered by point defects, which can generate a stress field in a crystal volume much larger than the defect itself, as illustrated by arrows in Figure 41. Point defects are of three types:
Vacancies and foreign atoms
Vacancies, characterized by the absence of an atom in a regular lattice site (A);
Interstitials, which occur when a small foreign atom (B) occupies empty spaces in the lattice. If a constituent atom of the crystal occupies such a site, it is called a self-interstitial (B’);
Substitutional atoms, which form when a foreign atom (C, C’) replaces a regular constituent atom of the crystal.

## Slide 5
Among these, vacancies are particularly significant because they facilitate the movement of atoms within the crystal a process known as "diffusion." This process largely controls the behavior of materials at high temperatures.
Vacancies and foreign atoms (2)

## Slide 6
In metals, point defects are typically produced independently of one another. In ionic crystals, however, electrical neutrality must be maintained and defects are created in pairs of opposite charges. Two main types of defects are observed:
Schottky defects, consisting of a paired anion vacancy and cation vacancy;
Frenkel defects, involving a vacancy (cationic or anionic) and an interstitial ion (anion or cation).
Ionic crystals
In Schottky defects, the vacancy left by a cation is negatively charged while the vacancy left by an anion is positively charged. In Frenkel defects, a negatively or positively charged vacancy is formed while the interstitial atom introduces an excess of positive or negative charge in that region of the crystal.